### PURPOSE

The purpose of determining biochar dry matter content (or moisture content) is to provide a standardized, accurate basis for measuring other critical properties (like carbon content, ash content, and nutrient levels) and to ensure accurate mass calculations for applications such as carbon sequestration and soil amendment.

This procedure document provides ArborX with a consistent method of determining biochar dry matter content in a manner that is aligned with the requirements of the Climate Action Reserve (CAR) Biochar Protocol and ISO 589.

### APPLICABILITY

This procedure must be applied for each shipment of ArborX biochar from which Climate Reserve Tonnes (“carbon removal credits”) are generated.

Note that this procedure does not apply to the CAR sampling requirements (Initial Parameter or Retention sampling) for determination of biochar quality, including organic carbon content and biochar H:Corg ratio. Biochar quality sampling requirements are addressed in ArborX Document 09 (“Biochar Quality Sampling Procedure”).

### BIOCHAR DRY MATTER CONTENT TESTING

## 3.1 Collection of a Representative Sample

The key to accurate results is obtaining a representative sample, as moisture content can be highly variable across a production batch or shipment load.

- Biochar Sampling: Biochar sub-samples should be collected as close as possible to the time a biochar shipment is weighed on the ArborX industrial truck scale. Collect a minimum of ten sub-samples from various locations and depths within the biochar shipment truckload using the following guidance to ensure representative sampling of biochar:

- If the truckload is well mixed, take samples from at least 10 different areas, ensuring that all samples are from at least 10 cm below the biochar surface

- If the truckload is not well mixed (and cannot easily be mixed), take four samples each from the top, middle, and bottom sections.

As much as possible the location of sub-sample collections should be based on a grid-based approach of the biochar shipment in the truckload to introduce randomness in the sampling.

- Creation of Composite Sample: Combine all sub-samples into a larger container and mix them thoroughly to create a homogenized, composite sample. The composite sample volume must be at least 2 liters.

- Preparation of Sample for Oven: The sub-tasks described below should be followed to prepare a sample for oven-drying:

- A sample of at least 600 grams should be extracted from the composite sample. Ensure that the sample does not overrepresent a specific particle size fraction. If the biochar is moist, collect a larger initial weight

- The sample should be crushed (if necessary) to ensure the nominal top size of biochar does not exceed 10 mm (0.4”)

- Packaging and Labeling of Oven Sample: Place the oven-ready sample in a sealed container (e.g., a reusable plastic bag) to prevent moisture change. Label it with the date and time of sampling and the ArborX Dry Matter Sample Number.

## 3.2 Dry Matter Content Testing

- Weigh an empty drying bowl or crucible with an accuracy of at least 0.1 g.

- Record the initial mass of the sample (at least 600 grams of biochar) and container to the nearest gram on the ArborX Dry Matter Content Sampling Form.

- Place the sample in a drying oven at a temperature of 110°C.

- Dry until the mass is constant for a minimum of 16 hours. The drying time only starts once the oven reaches the target temperature.

- Once drying and a constant mass is achieved, weigh the sample immediately after removal from the drying oven and record on the ArborX Dry Matter Content Sampling Form.

## 3.3 Calculations

The dry matter content (or moisture content) is calculated based on the mass lost during the drying process.

Dry Matter Content (%):   (Final Mass of Sample / Initial Mass of Sample) * 100%

Values of calculated dry matter content should be recorded on the ArborX Dry Matter Content Sampling Form.

### DATA RECORDING AND DOCUMENT RETENTION

ArborX has a Biochar Dry Matter Content Sample Form (ArborX  Document 08 - provided as an appendix to this procedure). This form must be completed for each delivery of biochar that leaves the facility. Note the calculated dry matter content will also be entered in the ArborX Biochar Output Delivery Form (ArborX Document 06).

Data from the Biochar Dry Matter Content Sample Forms will be entered to the Mangrove MRV system. The original completed forms will be stored at ArborX offices, with copies backed up on a secure remote data server.

### REFERENCES

ArborX Document 06 – Biochar Output Delivery Form

ArborX Document 08 – Biochar Dry Matter Content Sample Form

ArborX Document 09 - Biochar Quality Sampling Procedure

APPENDIX – Biochar Dry Matter Content Sample Form

- Date of Biochar Shipment (month/day/year): ______________________

- ArborX Biochar Shipment Number*: _________________________

*the biochar shipment number must match the value in the Biochar Output Delivery Form

- Number of sub-samples collected: ________________

- Time of sample collection: _________________

- ArborX Dry Matter Sample Number: __________________

- Initial (pre-drying) weight of sample for oven-drying (grams): ______________

- Time that oven drying was initiated: ________________

- Temperature of drying oven (Celsius): __________________

- Length of time drying in oven (hours + minutes): __________________

- Weight of sample after constant mass is achieved in oven (grams): _____________

- Biochar dry matter content* (%): ___________________

*Dry Matter Content (%):  (Final Mass of Sample / Initial Mass of Sample) * 100%

The U.S. and Canada Biochar Protocol (version 1.0) is published by the Climate Action Reserve and is available at https://climateactionreserve.org/how/protocols/ncs/biochar/. Biochar dry matter sampling requirements are addressed in Section 6.3.2 of the Protocol.

ISO 589: 2008 Hard Coal – Determination of total moisture.